Fiberglass RTP Pipe Production Line

For High Pressure Applications

### RTP Pipe Application

Reinforced thermalplastic pipe have been developed for high pressure pipeline, it is used in some applications to instead of the steel pipe because of its advantage of:

Anti-corrosive

Flexible

High pressure up to 19 MPa

Easy installation

General Introduction

High pressure fiberglass RTP pipe production line is xinrong’s another self-developed product after ten years’ of continuous research work and testing. This RTP pipe is reinforced by high strength fiberglass, customer could easily change for different number of fiberglass according to different pipe pressure rankings. It could be made up to 200bar (4 inches RTP pipe). This is an idea product for high pressure oil and gas application.

xinrong’s High pressure fiberglass RTP pipe meet International standards like ISO Draft TS 18226: “Reinforced thermoplastic piping systems for gaseous fuels” and API RP 15S, 1st Edition API Recommended Practice “Qualification of Reinforced Plastic Line Pipe” etc.

Structure of the pipe

The feature of pipe’s structure is 10 fiberglass reinforced layer.

Figure 1

Description

Pipe Specification

Fiberglass RTP pipe specification

| Pipe Size | OD (mm) | ID (mm) | Pressure (mpa) |
| --- | --- | --- | --- |
| 3 inches | 102 | 74 | More than 25 |
| 4 inches | 135 | 101 | More than 20 |
| 5 inches | 162 | 127 | More than 20 |
| 6 inches | 191 | 152 | More than17.5 |
| 8inchs |  |  | More than 17.5 |

RTP pipe jointing system

Xinrong  Company has developed crimp and expansion fittings which allows efficient joining directly to steel lines, standard flanged connections, or other RTP pipelines.

The xinrong  Company fitting is a metallic device that mechanically fastens to the pipe. The fitting can terminate the pipe with a standard ASME B16.5 lap-joint flange or a weld neck transition. The fitting consists of a mandrel which is inserted into the pipe, and a sleeve which is crimped around the pipe. The mandrel and sleeve are both equipped with uni-directional teeth that securely grip the liner and jacket of the pipe.

Fittings are installed using specialized installation equipment that energizes the fitting. The energizing force creates a clamping pressure that holds the pipe in place and provides a seal between the thermoplastic liner and the fitting. For additional seal reliability the fitting is equipped with two o-rings. The fitting system does not require the application of heat or adhesives.

Flanged end fitting

Prepare fitting and pipe               Pipe inserted into fitting by hydraulic device

Hydraulic crimping fitting sleeve                  Finished pipe fitting

Weld neck fitting

Prepare fitting and pipe               Pipe inserted into fitting by hydraulic device

Hydraulic crimping fitting sleeve                  Finished pipe fitting

Coupling fitting

Prepare coupling fitting and pipes         One pipe inserted into fitting

The other pipe inserted into fitting     Hydraulic crimping fitting sleeve for both sides

Finished pipe coupling fitting

Expansion steel pipe fitting

How the fitting is made by expansion method

Put steel fitting and taper rod on hydraulic device           Insert pipe

Put a steel sleeve outside of pipe and pull the taper            Finished pipe fitting

Cross section of the pipe fitting

Bursting pressure test

xinrong company have done countless tests for RTP pipe bursting pressure. Right now, it is easily to reach RTP bursting pressure at 400bar and above. It is no problem for even much higher pressure by simply increasing glass fiber numbers using xinrong’s new technology.

Pipe bursts at 400bar

RTP pipes used for bursting testing

Long time pressure holding test

Except short time bursting pressure, xinrong company have conducted its RTP pipe long time pressure holding test. We hold the pressure for 70 days at 200 bar, it proves there no any failure for both RTP pipes and fitting.

Holding pressure device                  Holding pressure at 200bar

General Requirement

- Applications:

RTP pipe for onshore and offshore

- Pipe Production Process

The machine is in two steps process.

First step is to produce the core tube for RTP pipe. And there is designed the co-extrusion in the core pipe, in case it needs to use the impermeable layer, then it can make the liner layer on the pipe.then move to the reinforced layer wrapping machine.

10 layers fiberglass reinforced layer is designed for RTP pipe. Every clockwise and anti-clockwise fiberglass winding unit combines a group of wrapping machine. A heating oven and an extruder is equipped between each two groups of wrapper for adhesive.

CAPACITY, DIMENSION AND POWER COMSUPTION

Production speed: 	2000 m/ 24 hours (6 inches pipe)

1.4m/min (6 inches pipe)

Workshop Dimension:   	130 X 18 X 7 (L W H)

Power supply:	380 KW

Practical power consumption:  	300KW

Water consumption:	12 m3/h

Air consumption:	1.0-1.5m3/min

Workers per shift:          	3

- GLASSFIBER TAPE SPECIFICATION

We will offer supplier ,price is cheaper

The treated fiberglass is provided by Chinese supplier in standard bobbins.

# Text boxes

Core Tube Extrusion

Material: PE

PE is used for liquid temperature no more than 90°C

Reinforced layer winding

Material: High strength fiberglass tape.

The fiber is wrapped alternated clockwise and anti-clockwise as a fixed spiral angle of 55°44’, the customer can select different layers fiber for different pressure.

Outer layer extrusion

Material: PE

Outside of pipe use PEF. If need the scratch proof ability, could make a thin PP protection layer.